## Slide 1: The basic design and operational characteristics of single-mode fibers.

## Slide 2
In the design of single-mode fibers, two factors are to be considered. These are
i) dispersion (ii) attenuation
For silica-based fibers the dispersion minimum is around 1.3 mm, whereas the attenuation minimum is around 1.55 mm

## Slide 3
For an ideal design, the dispersion minimum should be at the attenuation minimum.
In order to optimize the performance of single-mode fibers, therefore, a number of designs with different refractive index profiles for the core and cladding have been investigated.
The designs may be grouped into four categories:
(i) standard or conventional 1.3-mm optimized fibers
(ii) dispersion-shifted fibers (DSFs)
(iii) dispersion-flattened fibers (DFFs)
(iv) large effective area fibers (LEAFs)

## Slide 4: Dispersion Shifted Fiber
Dispersion Shifted Fiber is a type of single-mode optical fiber with a core-clad index profile tailored to shift the zero-dispersion wavelength from the natural 1300 nm in silica-glass fibers to the minimum-loss window at 1550 nm.
The group velocity or intramodal dispersion which dominates in single-mode fibers includes both material and waveguide dispersion.
Waveguide dispersion can be made more negative by changing the index profile and thus be used to offset the fixed material dispersion, shifting or flattening the overall intramodal dispersion.
This is advantageous because it allows a communication system to possess both low dispersion and low attenuation.

## Slide 5: Large effective area fibers
A singlemode, non-zero dispersion-shifted fiber with an effective area of 72
A singlemode, non-zero dispersion-shifted fiber with an effective area of 72 µm2 reduces nonlinear effects in long-haul transmission systems.
Large Effective Area Fiber (LEAF) is designed for use with dense WDM systems operating in the 1550 nm window at 10 Gbit/s.

## Slide 6: dispersion-flattened fibers (DFFs)
A type of Glass optical Fiber providing low pulse Dispersion over a broad portion of the Light spectrum. This means it can operate at 1300-nm and 1550-nm wavelengths simultaneously.

## Slide 7: Refractive-Index Profiles
When creating single-mode fibers, manufacturers pay special attention to how the fiber design affects both chromatic and polarization-mode dispersions.
Such considerations are important because these dispersions set the limits on long-distance and high-speed data transmission.
The chromatic dispersion of a step-index silica fiber is lowest at 1310 nm. However, if the goal is to transmit a signal as far as possible, it is better to operate the link at 1550 nm (in the C-band) where the fiber attenuation is lower.
For high-speed links the C-band presents a problem because chromatic dispersion is much larger at 1550 nm than at 1310 nm.
Consequently, fiber designers devised methods for adjusting the fiber parameters to shift the zero-dispersion point to longer wavelengths.

## Slide 8
The basic material dispersion is hard to alter significantly.
However, it is possible to modify the waveguide dispersion by changing from a simple step-index design to more complex index profiles for the cladding, thereby creating different chromatic-dispersion characteristics in single-mode fibers.
Popular single-mode fibers that are used widely in telecommunication networks are near-step-index fibers, which are optimized for use in the O-band around 1310 nm.
These 1310-nm-optimized single mode fibers are of either the matched-cladding or the depressed-cladding

## Slide 9
Matched-cladding fibers have a uniform refractive index throughout the cladding.
Typical mode-field diameters are 9.5 mm and the core-to-cladding index differences are around 0.35 percent.
In depressed-cladding fibers the cladding material next to the core has a lower index than the outer cladding region.
Mode-field diameters are around 9.0 mm, and typical positive and negative index differences are 0.25 and 0.12 percent, respectively

## Slide 10
Material dispersion depends only on the composition of the material, waveguide dispersion is a function of the core radius, the refractive index difference, and the shape of the refractive index profile.
Thus the waveguide dispersion can vary dramatically with the fiber design parameters.
By creating a fiber with a larger negative waveguide dispersion and assuming the same values for material dispersion as in a standard single-mode fiber, the addition of waveguide and material dispersion can then shift the zero dispersion point to longer wavelengths.
The resulting optical fiber is known as a dispersion-shifted fiber (DSF).

## Slide 11
The larger core areas reduce the effects of fiber nonlinearities, which limit system capacities of transmission systems that have densely spaced WDM channels.
Whereas standard single-mode fibers have effective core areas of about 55 mm2 , these profiles yield values greater than 100 mm2 .
An alternative fiber design concept is to distribute the dispersion minimum over a wider spectral range.
This approach is known as dispersion flattening. Dispersion-flattened fibers are more complex to design than dispersion-shifted fibers, because dispersion must be considered over a much broader range of wavelengths

## Slide 12: Dispersion Calculations
The total chromatic dispersion in single-mode fibers consists mainly of material and waveguide dispersions. The resultant intramodal or chromatic dispersion is represented by
where t is the group delay. The dispersion is commonly expressed in ps /(nm . km). The broadening of an optical pulse over a fiber of length L is given by
where is the half-power spectral width of the optical source.

## Slide 13: Mode-Field Diameter
One uses the mode field diameter in describing the functional properties of a single-mode fiber, since it takes into account the wavelength-dependent field penetration into the cladding.

## Slide 14: Bending Loss
Macro bending and micro bending losses are important in the design of single-mode fibers.
These losses are principally evident in the 1550-nm region and show up as a rapid increase in attenuation when the fiber is bent smaller than a certain bend radius.
The lower the cutoff wavelength relative to the operating wavelength, the more susceptible single-mode fibers are to bending.
The bending losses are primarily a function of the mode-field diameter. Generally, the smaller the mode-field diameter (i.e., the tighter the confinement of the mode to the core), the smaller the bending loss

## Slide 15
By specifying bend-radius limitations when installing standard single-mode fibers, one can largely avoid high micro bending losses.
Manufacturers usually recommend a fiber or cable bend diameter no smaller than 40–50 mm
This is consistent with bend diameter limitations of 50–75 mm specified by installation guides for cable placement in ducts, fiber-splice enclosures, and equipment racks.
The development of bend-insensitive fibers allows much tighter coiling of these fibers in optoelectronic packages. In addition, use of these bend-insensitive fibers in jumper cables greatly reduces bending loss effects when they are installed in highly confined equipment racks.